## Slide 1: LCLS-II High Q0 Cavities: Lessons Learned
Dan Gonnella
For the LCLS-II Project

## Slide 2: Outline
Overview of LCLS-II Cavity Requirements
Initial LCLS-II Results
Lesson Learned: Flux Expulsion
Lesson Learned: Nitrogen-Doping, RBCS
Vendor B Production Results
Lesson Learned: Vendor Oversight
Conclusions and Outlook

## Slide 3: Outline
Overview of LCLS-II Cavity Requirements
Initial LCLS-II Results
Lesson Learned: Flux Expulsion
Lesson Learned: Nitrogen-Doping, RBCS
Vendor B Production Results
Lesson Learned: Vendor Oversight
Conclusions and Outlook

## Slide 4: Introduction to LCLS-II
The SRF linac is closely based on the XFEL/ILC/TESLA Design
It consists of 35 cryomodules each with 8 cavities – total of 280 cavities
The 280 1.3 GHz 9-cell cavities have a very ambitious Q specification:
Additionally, cavities must reach 19 MV/m
2.7 x 1010 at 16 MV/m and 2 K
2.5 x 1010 at 16 MV/m and 2 K
Q specification lowered in VT due to addition of stainless steel blank on short side of cavity – adds ~0.8 nΩ of Rres

## Slide 5: Cavity Preparation
In order to achieve the ambitious Q specification, all 9-cell cavities for LCLS-II are prepared with nitrogen-doping
Original recipe:
  140 μm bulk EP
  800oC degas for 3 hours in vacuum
  2 minutes at 800oC in 20-30 mTorr of N2
  6 minutes at 800oC in vacuum
  5-7 μm light EP

## Slide 6: Cavity Preparation
In order to achieve the ambitious Q specification, all 9-cell cavities for LCLS-II are prepared with nitrogen-doping
Original recipe:
  140 μm bulk EP
  800oC degas for 3 hours in vacuum
  2 minutes at 800oC in 20-30 mTorr of N2
  6 minutes at 800oC in vacuum
  5-7 μm light EP

## Slide 7: Cavity Preparation
In order to achieve the ambitious Q specification, all 9-cell cavities for LCLS-II are prepared with nitrogen-doping
Original recipe:
  140 μm bulk EP
  800oC degas for 3 hours in vacuum
  2 minutes at 800oC in 20-30 mTorr of N2
  6 minutes at 800oC in vacuum
  5-7 μm light EP
Cavities are being produced by Research Instruments GmbH (RI) and Ettore Zanon S.p.a (EZ)
Niobium was procured from Tokyo Denkai and OTIC Ningxia

## Slide 8: Nitrogen-Doping Introduction

## Slide 9: Nitrogen-Doping Introduction
Q is improved by 2 mechanisms:
  Higher starting Q0
  Anti-Q slope
Both of these are a resulting of a changing RBCS
Q0’s of >3x1010 can consistently be produced

## Slide 10: Anti-Q Slope
Anti-Q Slope caused by a decreasing RBCS
Vendor Qualification Cavities
Low RBCS and anti-Q slope are characteristic of nitrogen-doped cavities

## Slide 11: Drawbacks of N-Doping
Q0 is significantly improved by the lowering of RBCS
There is a tradeoff however with Rres
Nitrogen-doped cavities are more sensitive to losses from trapped magnetic flux
For the same amount of trapped flux, a N-doped cavity will have a higher Rres than an un-doped cavity
  3.4x for the LCLS-II cavity recipe
This requires efficient flux expulsion or small ambient magnetic fields to maintain high Q0
Presented at SRF 2015 and J. Appl. Phys. 119:073904

## Slide 12: Outline
Overview of LCLS-II Cavity Requirements
Initial LCLS-II Results
Lesson Learned: Flux Expulsion
Lesson Learned: Nitrogen-Doping, RBCS
Vendor B Production Results
Lesson Learned: Vendor Oversight
Conclusions and Outlook

## Slide 13: Q vs E for First Article Cavities
Some Great Cavities
Some Good Cavities
All these cavities tested in very low (0-1 mG) magnetic fields

## Slide 14: Residual Resistance in First Articles
Rres higher than in the prototyping phase
Expected 2-3 nΩ, found 5-9 nΩ
Spread is a result of differences in ambient magnetic fields

## Slide 15: Outline
Overview of LCLS-II Cavity Requirements
Initial LCLS-II Results
Lesson Learned: Flux Expulsion
Lesson Learned: Nitrogen-Doping, RBCS
Vendor B Production Results
Lesson Learned: Vendor Oversight
Conclusions and Outlook

## Slide 16: Flux Expulsion in Production Material
As received material for LCLS-II Production
After 900oC Heat Treatment
Slide from S. Posen, TTC 2017
With the 800oC recipe, flux expulsion was much worse than on the prototype material
Raising the temperature to 900oC significantly improved flux expulsion

## Slide 17: Issues with Original Recipe
Material from both vendors showed worse flux expulsion when treated at 800oC in single-cell cavity tests than material used during the prototyping and R&D stage
  All material meets specifications
This means that magnetic field specifications would need to be tighter in order to minimize the need for efficient flux expulsion
Cryomodule results thus far have shown ambient magnetic fields less than the LCLS-II CM Spec of 5 mG – further improvement on this would be difficult
140 μm bulk EP was insufficient to remove the damage layer, adding additional Rres
Worse flux expulsion is an independent phenomena from N-Doping – It impacts all cavity preparation methods

## Slide 18: Cavity Preparation
In order to achieve the ambitious Q specification, all 9-cell cavities for LCLS-II are prepared with nitrogen-doping
Updated recipe:
  200 μm bulk EP
  900oC degas for 3 hours in vacuum
  2 minutes at 800oC in 20-30 mTorr of N2
  6 minutes at 800oC in vacuum
  5-7 μm light EP

## Slide 19: Residual Resistance in First Articles

## Slide 20: Residual Resistance After Recipe Change
After Increasing Bulk EP and Degas Temperature,
Rres is consistently ~2 nΩ
Spread lower due to near 100% FE

## Slide 21: Q vs E for First Article Cavities

## Slide 22: Q vs E for First Article Cavities
Cavities now consistently meet Q0 specification

## Slide 23
Cavities now consistently meet Q0 specification
Lesson 1: Efficient flux expulsion is necessary to maintain High Q0 in N-Doped Cavities

## Slide 24: Outline
Overview of LCLS-II Cavity Requirements
Initial LCLS-II Results
Lesson Learned: Flux Expulsion
Lesson Learned: Nitrogen-Doping, RBCS
Vendor B Production Results
Lesson Learned: Vendor Oversight
Conclusions and Outlook

## Slide 25: Reminder: Anti-Q Slope
Vendor Qualification Cavities

## Slide 26: RBCS in Production Cavities
Strong Anti-Q Slope
Decreasing RBCS from ~7 to ~4 nΩ
Production cavities show similar anti-Q slope to R&D cavities

## Slide 27: RBCS in Production Cavities
RBCS at 16 MV/m and 2.0 K is consistently 4-6 nΩ
This is consistent with “2/6” N-Doping developed in the R&D phase of LCLS-II
Mix of Material from 3 Vendors
RBCS consistently between 4 and 6 nΩ at 16 MV/m

## Slide 28
RBCS at 16 MV/m and 2.0 K is consistently 4-6 nΩ
This is consistent with “2/6” N-Doping developed in the R&D phase of LCLS-II
Mix of Material from 3 Vendors
RBCS consistently between 4 and 6 nΩ at 16 MV/m
Lesson 2: The Nitrogen-Doping process can be successfully carried out at cavity vendors

## Slide 29: Outline
Overview of LCLS-II Cavity Requirements
Initial LCLS-II Results
Lesson Learned: Flux Expulsion
Lesson Learned: Nitrogen-Doping, RBCS
Vendor B Production Results
Lesson Learned: Vendor Oversight
Conclusions and Outlook

## Slide 30: Vendor B: Q0 Results
Vendor B has completed fabrication of original order of 133 cavities
128 cavities have been tested so far at JLab and Fermilab

## Slide 31: Vendor B: Q0 Results
Vendor B has completed fabrication of original order of 133 cavities
128 cavities have been tested so far at JLab and Fermilab
TD Cavities 900/200 preparation consistently exceed LCLS-II spec

## Slide 32: Vendor B: Q0 Results
Vendor B has completed fabrication of original order of 133 cavities
128 cavities have been tested so far at JLab and Fermilab
TD Cavities 900/200 preparation consistently exceed LCLS-II spec
NX Cavities at 900oC have middling results

## Slide 33: Vendor B: Q0 Results
Vendor B has completed fabrication of original order of 133 cavities
128 cavities have been tested so far at JLab and Fermilab
TD Cavities 900/200 preparation consistently exceed LCLS-II spec
NX Cavities at 900oC have middling results
950 and 975oC have further improved upon the NX cavities’ performance

## Slide 34: Vendor B Results
JLab employs an administrative limit at 24 MV/m during VT
Gradient reach has consistently exceeded specification throughout production

## Slide 35: Outline
Overview of LCLS-II Cavity Requirements
Initial LCLS-II Results
Lesson Learned: Flux Expulsion
Lesson Learned: Nitrogen-Doping, RBCS
Vendor B Production Results
Lesson Learned: Vendor Oversight
Conclusions and Outlook

## Slide 36: Vendor A Results
Vendor A cavities were dominated by a strong Q slope with onset 12-16 MV/m
This Q slope led to early quench and low Q at 16 MV/m
Q Slope Onset 12-14 MV/m
Subset of cavities, behavior observed in most

## Slide 37: Vendor A – Surface Roughness
EP at Vendor A was producing a very rough surface
Roughness was as high as 15 μm
It was found that EP temperature was leading to the EP no longer being in the “polishing regime” but in the “etching regime”
This Issue was Fixed
Data from Y. Trenikhina

## Slide 38: Vendor A – Surface Roughness
3 of 4 cavities with “New EP” still had strong Q slope
Bad EP was not the cause of the performance issues
Q Slope Still Present after EP Procedure Change

## Slide 39: Vendor A – Grinding Technique
Visual inspection of the interior of Vendor A cavities after fabrication showed the presence of many defects
Some pits had visible normal conducting media embedded
Theorized that aggressive grinding on the dumbbell surface led to the “burying” of media
This normal conducting media would then be revealed after bulk EP
All procedures were reworked with LCLS-II staff to improve the fabrication procedures

## Slide 40: Vendor A – Restart
13 cavities with new grinding techniques have been tested
No evidence of Q slope that was seen before
4 of the 13 still had quench fields below 19 MV/m
After these 13 cavities, a new weld stack-up procedure was implemented

## Slide 41: Vendor A - Restart
Cavities prepared with original grinding had poor gradient reach

## Slide 42: Vendor A - Restart
Cavities prepared with original grinding had poor gradient reach
Cavities with new grinding had better gradient reach but cavities were still limited

## Slide 43: Vendor A - Restart
Cavities prepared with original grinding had poor gradient reach
Cavities with new grinding had better gradient reach but cavities were still limited
Almost all cavities with new weld stack-up meet gradient spec

## Slide 44
Cavities prepared with original grinding had poor gradient reach
Cavities with new grinding had better gradient reach but cavities were still limited
Almost all cavities with new weld stack-up meet gradient spec
Lesson 3: Oversight at the cavity vendors is crucial to maintaining performance

## Slide 45: Outline
Overview of LCLS-II Cavity Requirements
Initial LCLS-II Results
Lesson Learned: Flux Expulsion
Lesson Learned: Nitrogen-Doping, RBCS
Vendor B Production Results
Lesson Learned: Vendor Oversight
Conclusions and Outlook

## Slide 46: Conclusions and Outlook
LESSON 1: Efficient flux expulsion is necessary to maintain High Q0 in N-Doped Cavities
  A recipe change mid-production was necessary to improve flux expulsion
  Cavities now consistently reach >3x1010
LESSON 2: The Nitrogen-Doping process can be successfully carried out at cavity vendors
  RBCS in production cavities is consistent with those from the R&D phase
LESSON 3: Oversight at the cavity vendors is crucial to maintaining performance
  One of the cavity vendors had many issues in regards to cavity grinding, improper EP, and poor weld stack-up procedures which led to limited gradient reach in cavities
  New procedures have brought Vendor A cavity performance in line with that of Vendor B

## Slide 47
Questions?