## Slide 1: Results and New Insights from Vertical Testing of LCLS-II Production Cavities
Dan Gonnella
For the LCLS-II Project

## Slide 2: Outline
Overview of LCLS-II Cavity Requirements
First Article Results
  Change of Recipe
RBCS in Production Cavities
Production Results
Conclusions and Outlook

## Slide 3: Outline
Overview of LCLS-II Cavity Requirements
First Article Results
  Change of Recipe
RBCS in Production Cavities
Production Results
Conclusions and Outlook

## Slide 4: Introduction to LCLS-II
The SRF linac is closely based on the XFEL/ILC/TESLA Design
It consists of 35 cryomodules each with 8 cavities – total of 280 cavities
The 280 1.3 GHz 9-cell cavities have a very ambitious Q specification:
Additionally, cavities must reach 19 MV/m
2.7 x 1010 at 16 MV/m and 2 K
2.5 x 1010 at 16 MV/m and 2 K
Q specification lowered in VT due to addition of stainless steel blank on short side of cavity – adds ~0.8 nΩ of Rres

## Slide 5: Cavity Preparation
In order to achieve the ambitious Q specification, all 9-cell cavities for LCLS-II are prepared with nitrogen-doping
Original recipe:
  140 μm bulk EP
  800oC degas for 3 hours in vacuum
  2 minutes at 800oC in 20-30 mTorr of N2
  6 minutes at 800oC in vacuum
  5-7 μm light EP

## Slide 6: Cavity Preparation
In order to achieve the ambitious Q specification, all 9-cell cavities for LCLS-II are prepared with nitrogen-doping
Original recipe:
  140 μm bulk EP
  800oC degas for 3 hours in vacuum
  2 minutes at 800oC in 20-30 mTorr of N2
  6 minutes at 800oC in vacuum
  5-7 μm light EP

## Slide 7: Cavity Preparation
In order to achieve the ambitious Q specification, all 9-cell cavities for LCLS-II are prepared with nitrogen-doping
Original recipe:
  140 μm bulk EP
  800oC degas for 3 hours in vacuum
  2 minutes at 800oC in 20-30 mTorr of N2
  6 minutes at 800oC in vacuum
  5-7 μm light EP
Cavities are being produced by Research Instruments GmbH (RI) and Ettore Zanon S.p.a (EZ)
Niobium was procured from Tokyo Denkai and OTIC Ningxia

## Slide 8: Nitrogen-Doping Introduction

## Slide 9: Nitrogen-Doping Introduction
Q is improved by 2 mechanisms:
  Higher starting Q0
  Anti-Q slope
Both of these are a resulting of a changing RBCS
Q0’s of >3x1010 can consistently be produced

## Slide 10: Anti-Q Slope
Anti-Q Slope caused by a decreasing RBCS
Vendor Qualification Cavities

## Slide 11: Drawbacks of N-Doping
Q0 is significantly improved by the lowering of RBCS
There is a tradeoff however with Rres
Nitrogen-doped cavities are more sensitive to losses from trapped magnetic flux
For the same amount of trapped flux, a N-doped cavity will have a higher Rres than an un-doped cavity
  3.4x for the LCLS-II cavity recipe
This requires efficient flux expulsion or small ambient magnetic fields to maintain high Q0
Presented at SRF 2015 and J. Appl. Phys. 119:073904
See Also:
A. Palczewski TUXBA06
S. Posen TUXBA02
J. Maniscalco TUYAA01

## Slide 12: Outline
Overview of LCLS-II Cavity Requirements
First Article Results
  Change of Recipe
RBCS in Production Cavities
Production Results
Conclusions and Outlook

## Slide 13: Q vs E for First Article Cavities
Some Great Cavities
Some Good Cavities
All these cavities tested in very low (0-1 mG) magnetic fields

## Slide 14: Residual Resistance in First Articles
Rres higher than in the prototyping phase
Expected 2-3 nΩ, found 5-9 nΩ
Spread is a result of differences in ambient magnetic fields

## Slide 15: Issues with Original Recipe
Material from both vendors showed worse flux expulsion when treated at 800oC in single-cell cavity tests than material used during the prototyping and R&D stage
  All material meets specifications
This means that magnetic field specifications would need to be tighter in order to minimize the need for efficient flux expulsion
Cryomodule results thus far have shown ambient magnetic fields less than the LCLS-II CM Spec of 5 mG – further improvement on this would be difficult
140 μm bulk EP was insufficient to remove the damage layer, adding additional Rres
Worse flux expulsion is an independent phenomena from N-Doping – It impacts all cavity preparation methods

## Slide 16: Outline
Overview of LCLS-II Cavity Requirements
First Article Results
  Change of Recipe
RBCS in Production Cavities
Production Results
Conclusions and Outlook

## Slide 17: Cavity Preparation
In order to achieve the ambitious Q specification, all 9-cell cavities for LCLS-II are prepared with nitrogen-doping
Updated recipe:
  200 μm bulk EP
  900oC degas for 3 hours in vacuum
  2 minutes at 800oC in 20-30 mTorr of N2
  6 minutes at 800oC in vacuum
  5-7 μm light EP
For additional information see:
A. Palczewski TUXBA06
S. Posen TUXBA02

## Slide 18: Residual Resistance in First Articles

## Slide 19: Residual Resistance After Recipe Change
After Increasing Bulk EP and Degas Temperature,
Rres is consistently ~2 nΩ
Spread lower due to near 100% FE

## Slide 20: Q vs E for First Article Cavities

## Slide 21: Q vs E for First Article Cavities
Cavities now consistently meet Q0 specification
Highest Q0 Ever Obtained in Production SRF Cavities

## Slide 22: Outline
Overview of LCLS-II Cavity Requirements
First Article Results
  Change of Recipe
RBCS in Production Cavities
Production Results
Conclusions and Outlook

## Slide 23: Reminder: Anti-Q Slope
Vendor Qualification Cavities

## Slide 24: RBCS in Production Cavities
Strong Anti-Q Slope
Decreasing RBCS from ~7 to ~4 nΩ
Production cavities show similar anti-Q slope to R&D cavities

## Slide 25: RBCS in Production Cavities
RBCS at 16 MV/m and 2.0 K is consistently 4-6 nΩ
This is consistent with “2/6” N-Doping developed in the R&D phase of LCLS-II
Mix of Material from 3 Vendors
RBCS consistently between 4 and 6 nΩ at 16 MV/m

## Slide 26: Outline
Overview of LCLS-II Cavity Requirements
First Article Results
  Change of Recipe
RBCS in Production Cavities
Production Results
Conclusions and Outlook

## Slide 27: Vendor B Results
Vendor B has completed fabrication of original order of 133 cavities
99 cavities have been tested so far at JLab and Fermilab

## Slide 28: Vendor B Results
Vendor B has completed fabrication of original order of 133 cavities
99 cavities have been tested so far at JLab and Fermilab
TD Cavities 900/200 preparation consistently exceed LCLS-II spec

## Slide 29: Vendor B Results
Vendor B has completed fabrication of original order of 133 cavities
99 cavities have been tested so far at JLab and Fermilab
TD Cavities 900/200 preparation consistently exceed LCLS-II spec
NX Cavities have middling results with Q0’s ranging from 2 to 3x1010
  Future NX cavities will be treated at 950oC – evidence suggests this improves Qo

## Slide 30: Vendor B Results
JLab employs an administrative limit at 24 MV/m during VT
Gradient reach has consistently exceeded specification throughout production

## Slide 31: Vendor A Results
Vendor A cavities were dominated by a strong Q slope with onset 12-16 MV/m
This Q slope led to early quench and low Q at 16 MV/m
Q Slope Onset 12-14 MV/m
Subset of cavities, behavior observed in most

## Slide 32: Vendor A – Surface Roughness
EP at Vendor A was producing a very rough surface
Roughness was as high as 15 μm
It was found that EP temperature was leading to the EP no longer being in the “polishing regime” but in the “etching regime”
This Issue was Fixed
Data from Y. Trenikhina

## Slide 33: Vendor A – Surface Roughness
3 of 4 cavities with “New EP” still had strong Q slope
Bad EP was not the cause of the performance issues
Q Slope Still Present after EP Procedure Change

## Slide 34: Vendor A – Grinding Technique
Visual inspection of the interior of Vendor A cavities after fabrication showed the presence of many defects
Some pits had visible normal conducting media embedded
Theorized that aggressive grinding on the dumbbell surface led to the “burying” of media
This normal conducting media would then be revealed after bulk EP
All procedures were reworked with LCLS-II staff to improve the fabrication procedures

## Slide 35: Vendor A – Restart
7 cavities have been tested so far after restart
No evidence of Q slope that was seen before
2 of the 7 still have lower than ideal quench fields – may be related to expected spread

## Slide 36: Outline
Overview of LCLS-II Cavity Requirements
First Article Results
  Change of Recipe
RBCS in Production Cavities
Production Results
Conclusions and Outlook

## Slide 37: Conclusions and Outlook
Production of cavities for LCLS-II is well underway
The original recipe used caused poor flux expulsion and higher residual resistance than expected leading to a recipe change
With the new recipe TD cavities routinely reach >3x1010 at 16 MV/m
NX cavities still produce middling results: all future NX cavities will be heat treated at higher temperature

## Slide 38: Conclusions and Outlook
Production of cavities for LCLS-II is well underway
The original recipe used caused poor flux expulsion and higher residual resistance than expected leading to a recipe change
With the new recipe TD cavities routinely reach >3x1010 at 16 MV/m
NX cavities still produce middling results: all future NX cavities will be heat treated at higher temperature
Q0 at 16 MV/m

## Slide 39: Conclusions and Outlook
Production of cavities for LCLS-II is well underway
The original recipe used caused poor flux expulsion and higher residual resistance than expected leading to a recipe change
With the new recipe TD cavities routinely reach >3x1010 at 16 MV/m
NX cavities still produce middling results: all future NX cavities will be heat treated at higher temperature
Vendor B consistently produces cavities with great Q0 and quench fields
Vendor A has had issues with improper EP parameters, and a grinding technique that led to a strong Q slope
LCLS-II staff oversight and rework at Vendor A has improved performance – Vendor A now produces good cavities
Maximum Gradient

## Slide 40: Lessons Learned So Far
When dealing with high Q0 great care needs to be taken to maintain performance
Flux expulsion is especially important in Nitrogen-Doped cavities
Changes to cavity preparation recipe has been necessary at multiple stages to ensure performance is kept high
In order to meet schedule demands, some cavities will have worse flux expulsion than others
  Retreating all cavities is not a feasible option
Project oversight at cavity vendors is important
However when great care is taken…
We Can Obtain World Record Q0 in Production

## Slide 41
Questions?