## Slide 1: Impact of Cool-Down Procedure and Residual Field on High Q0 at Cornell
Dan Gonnella
For the Cornell Team
TTC Meeting
December, 2014

## Slide 2: Main Conclusions
Trapped flux contributes stronger to residual losses in nitrogen-doped cavities than in EP+120oC baked cavities.
Large spatial temperature gradients at the transition temperature reduce flux trapping, which can mitigate the above effect.
Thermal currents exist and can have an impact on cavity Q0.
Practical Advice:
  For best performance in cryomodule, cool down cavities with large transverse temperature gradients and small longitudinal temperature gradients.

## Slide 3: Single-Cell Studies
Cornell nitrogen-doped 5 single-cell ILC shaped cavities.
These 5 cavities along with a nitrogen-doped cavity from FNAL, and EP cavity , and an EP+120oC baked cavity were tested at Cornell.
  Residual resistance was measured for a variety of cool down rates, spatial gradients, and applied external magnetic field.
Notes: Table showing single and 9 cells

## Slide 4: Experimental Setup
Temperature Sensors
Fluxgate
Magnetometer
Helmholtz
Coil
Slow Cool
Down System

## Slide 5: The HTC
The Cornell Horizontal Test Cryomodule (HTC) is a full cryomodule that can hold one 9-cell cavity.
Ambient magnetic fields are ~2 mG with 2 layers of magnetic shielding.
Two 9-cell nitrogen doped cavities have been tested so far in the HTC.
Temperature Sensors
Notes: Very similar to LCLS-II cryomodule. 2 m section of the LCLS-II cryomodule. This is different than the HTS at FNAL or Jlab
Label things

## Slide 6: HTC Instrumentation
CNX Sensor
CNX Sensor
CNX Sensor
CNX Sensor
Fluxgate
Fluxgate
Fluxgate
Fluxgate
(transverse)
Heater on Beam Tube
Solenoid Around Cavity
Thanks to FNAL for providing fluxgates and CNX sensors.

## Slide 7: Main Conclusions
Trapped flux contributes stronger to residual losses in nitrogen-doped cavities than in EP+120oC baked cavities.
Large spatial temperature gradients at the transition temperature reduce flux trapping, which can mitigate the above effect.
Thermal currents exist and can have an impact on cavity Q0.
Practical Advice:
  For best performance in cryomodule, cool down cavities with large transverse temperature gradients and small longitudinal temperature gradients.

## Slide 8: Fluxgate Measurements
External Field Off
External Field Off,
Flux Trapped
External Field On
TC

## Slide 9: Rres vs Trapped Flux
Notes: Add arrow that shows what types of cavities

## Slide 10: Sensitivity to Ambient Fields
Nitrogen-doped cavities are significantly more susceptible to residual losses from trapped flux than EP and EP+120oC baked cavities.
Less nitrogen-doping results in less sensitivity.
There is ~2-4 nΩ of additional residual resistance per mG of trapped magnetic field in nitrogen-doped cavities.

## Slide 11: Solenoid Studies in the HTC
A solenoid was placed around the second HTC cavity, outside the helium vessel to induce an uniform external longitudinal field.
A field of ~10 mG was applied during a fast and slow cool down to study sensitivity to ambient magnetic fields.

## Slide 12: HTC Results
ΔRres=4.6 nΩ
ΔRres=36 nΩ
Cool Down | Solenoid On | Heater Used | ΔTlong [K] | ΔTtrans [K] | Blong (10 K) [mG] | Bperp (10 K) [mG] | Q0 (2 K, 16 MV/m) | Rres (16 MV/m) [nΩ] | RBCS (16 MV/m) [nΩ]
Fast 2 | No | No | 6.8 | 8.9 | 1.2 | 0.3 | 2.7x1010 | 4.5 | 5.8
Fast 3 | Yes | No | 5.9 | 7.0 | 10.1 | 7.2 | 1.9x1010 | 9.1 | 5.4
Slow 1 | Yes | No | 0.2 | 0.5 | 10.6 | 1.0 | 6.2x109 | 40.5 | 4.5

## Slide 13: ΔRres from External B
For slow cool down (ΔTtransverse= 0.5 K):
  This is consistent with Single-cell flux trapping measurements for strongly doped cavities.
For fast cool down (ΔTtransverse= 7 K):

## Slide 14: Main Conclusions
Trapped flux contributes stronger to residual losses in nitrogen-doped cavities than in EP+120oC baked cavities.
Large spatial temperature gradients at the transition temperature reduce flux trapping, which can mitigate the above effect.
Thermal currents exist and can have an impact on cavity Q0.
Practical Advice:
  For best performance in cryomodule, cool down cavities with large transverse temperature gradients and small longitudinal temperature gradients.

## Slide 15: Rres vs Cool Down Rate
Residual Resistance (normalized to ambient magnetic field) vs Spatial Gradient and Cool Down Rate
Above a threshold gradient, residual resistance decreases with larger gradient due to higher flux expulsion.
The trend is not as pronounced with cool down rate.
Larger spatial temperature gradient is better for high Q0.
Notes: Clearer correlation with gradient than rate.

## Slide 16: A Typical Cool Down in the HTC
With an ILC tank:
The cavity cools from the bottom first.
Cell 5 cools first, cell 1 follows shortly after.
The top of cells 5 and 1 cool next.
The top of cell 9 cools last, significantly later.
Helium Inlet
Chimney
The time it takes between the first sensor going through TC and a given sensor going through TC

## Slide 17: Q0 vs E Dependence on Gradient
Larger transverse temperature gradients result in higher Q0 (lower residual resistance)
Notes: All at mostly the same speed (at speed) increase symbol size maybe change color

## Slide 18: Main Conclusions
Trapped flux contributes stronger to residual losses in nitrogen-doped cavities than in EP+120oC baked cavities.
Large spatial temperature gradients at the transition temperature reduce flux trapping, which can mitigate the above effect.
Thermal currents exist and can have an impact on cavity Q0.
Practical Advice:
  For best performance in cryomodule, cool down cavities with large transverse temperature gradients and small longitudinal temperature gradients.

## Slide 19: Heater Studies
A heater was installed on one cell 9 beam tube in order to induce a large longitudinal thermal gradient.
  Hope was that this will reduce flux trapping and improve Q0
Heat this end
Cool from this end
Cryo inlet

## Slide 20: Fast Cool-Down with and without Beam Tube Heater
Without Heater
With Heater
Larger longitudinal (horizontal) T!

## Slide 21: Heater Studies, cont.
Cool Down | Solenoid On | Heater Used | ΔTlong [K] | ΔTtrans [K] | Blong (10 K) [mG] | Bperp (10 K) [mG] | Q0 (2 K, 16 MV/m) | Rres (16 MV/m) [nΩ] | RBCS (16 MV/m) [nΩ]
Fast 2 | No | No | 6.8 | 8.9 | 1.2 | 0.3 | 2.7x1010 | 4.5 | 5.8
Fast 4 | No | Yes, 50 W | 21.8 | 32.5 | 2.5 | 50.3 | 2.1x1010 | 7.3 | 6.0
Fast 6 | No | Yes, 100 W | 29.4 | 39.4 | 3.1 | 62.8 | 1.5x1010 | 11.9 | 6.3
Experiment:
Larger longitudinal T gives lower Q0 in a cryomodule!

## Slide 22
What we’ve seen so far:
  Transverse gradients are good.
  Longitudinal gradients are bad.
Why?

## Slide 23: Fast Cool-Down with and without Beam Tube Heater
Without Heater
With 50 W Heater
Large difference in transverse magnetic field!
Larger longitudinal (horizontal) T

## Slide 24: Heater Studies: Why Q0 went down
Larger horizontal temperature gradient:
Horizontal T drives thermal current
Current produces large transverse magnetic field
In vertical tests, rotational symmetry of the cavity results in no magnetic fields at inner cavity surface
BUT: In horizontal cavity tests, symmetry is broken due to vertical temperature gradients!!

## Slide 25: Thermal Currents in VT vs HT
THOT
TCOLD
i
Vertical Test
Cylindrical symmetry results in no magnetic field at cavity inner surface
Horizontal Test
TCOLD
THOT
i
i1
i2
Cavity cools from bottom and conductivity = (T)
Cylindrical symmetry is broken by transverse (vertical) temperature gradient and current will preferentially flow through the bottom of the cavity.
This results in a non-zero magnetic field at the cavity inner surface.
Magnetic fields from thermal currents are important in horizontal test!
i

## Slide 26: Heater Studies
Larger longitudinal temperature gradient causes a larger perpendicular magnetic field by thermal currents.
Larger perpendicular magnetic field causes significant increases in Rres even with large transverse gradients (unlike in vertical test).

## Slide 27: Main Conclusions
Trapped flux contributes stronger to residual losses in nitrogen-doped cavities than in EP+120oC baked cavities.
Large spatial temperature gradients at the transition temperature reduce flux trapping, which can mitigate the above effect.
Thermal currents exist and can have an impact on cavity Q0.
Practical Advice:
  For best performance in cryomodule, cool down cavities with large transverse temperature gradients and small longitudinal temperature gradients.

## Slide 28
Thank you for your attention!
Two papers on these topics on arXiv:
Nitrogen-Doped 9-Cell Cavity Performance in a Test Cryomodule for LCLS-II. D. Gonnella et. al. arXiv: 1411.1659
Thermocurrents and their Role in high Q Cavity Performance. R. Eichhorn et. al. arXiv: 1411.5285

## Slide 29: A Typical Cool Down in the HTC

## Slide 30: Fast Cool Down Dynamics
Fast cool-down with speeds similar to cool-down in vertical tests.
Low magnetic fields, including low transverse fields by thermal currents
Relative small horizontal temperature gradients (good, see later)
Relative large vertical temperature gradients (good, see later)
Fluxgates parallel to cavity axis
Fluxgate perpendicular to cavity axis
Note: Rates and gradients are defined for when that given sensor goes through TC