## Slide 1: Possible Field Dependence of Superconducting Properties in N-Doped Cavities
Dan Gonnella
Cornell University
December 1, 2015

## Slide 2: Outline
Deconvolution of Rres and RBCS
Fitting of field dependent data:
  Exponential fitting
  BCS fitting with SRIMP
  Fitting with Xiao code
Magnetic Field Studies
Conclusions

## Slide 3: Outline
Deconvolution of Rres and RBCS
Fitting of field dependent data:
  Exponential fitting
  BCS fitting with SRIMP
  Fitting with Xiao code
Magnetic Field Studies
Conclusions

## Slide 4: Surface Resistance
RBCS can be approximated as an exponential

## Slide 5: Deconvolution of Rres and RBCS
Both Rres and RBCS have been shown to be field dependent:

## Slide 6: Deconvolution in 120oC Cavities
Medium Field Q Slope
Medium field Q slope caused by a combination of increasing residual and BCS resistances in 120oC baked cavities

## Slide 7: Deconvolution in N-Doped Cavities
Anti-Q Slope
Anti-Q slope caused by a decreasing BCS resistance in N-Doped Cavities

## Slide 8: Outline
Deconvolution of Rres and RBCS
Fitting of field dependent data:
  Exponential fitting
  BCS fitting with SRIMP
  Fitting with Xiao code
Magnetic Field Studies
Conclusions

## Slide 9: Exponential Fitting
The usual BCS equation for fitting:
Both A and ε can vary with Eacc however fitting both together leads to sloppy fitting.

## Slide 10: Cavity LT1-3
1.3 GHz Single Cell ILC shaped cavity: bulk VEP, 800oC bake in vacuum for 3 hours, 20 min in 60 mTorr of N2 for 20 minutes, 30 minute anneal, 12 µm VEP

## Slide 11: Exponential Fitting
Both models can fit the RBCS data well in the anti-Q slope region

## Slide 12: Exponential Fitting

## Slide 13: Exponential Fitting

## Slide 14: Exponential Fitting
Fits with both A and ε field dependent are sloppy
Individual fits however can fit RBCS vs Eacc data very well
A decreasing A with field or an increasing ε can explain the anti-Q slope observed in N-doped cavities

## Slide 15: Outline
Deconvolution of Rres and RBCS
Fitting of field dependent data:
  Exponential fitting
  BCS fitting with SRIMP
  Fitting with Xiao code
Magnetic Field Studies
Conclusions

## Slide 16: BCS Fitting with SRIMP
SRIMP, a code written by Halbritter, can be used to calculate RBCS based on material parameters
  Tc, Mean Free Path, ε/kBTc, coherence length, and penetration depth
Low Field Fit of Q vs T

## Slide 17: BCS Fitting with SRIMP

## Slide 18: BCS Fitting with SRIMP
Energy Gap vs Eacc
Increasing Gap in the Medium Field Region

## Slide 19: BCS Fitting with SRIMP
RBCS vs Mean Free Path

## Slide 20: BCS Fitting with SRIMP
N-Doped cavities are on both sides of the RBCS vs Mean free path minimum
Increasing or decreasing mean free path with field alone cannot explain the anti-Q slope
RBCS vs Mean Free Path

## Slide 21: BCS Fitting with SRIMP
Field dependence of BCS resistance in N-Doped cavities is related to the energy gap
Nitrogen-doped cavities have mean free paths that are on both sides of the RBCS vs mean free path minimum
  An increasing or decreasing mean free path with accelerating field cannot explain a decreasing BCS resistance in all cavities

## Slide 22: Outline
Deconvolution of Rres and RBCS
Fitting of field dependent data:
  Exponential fitting
  BCS fitting with SRIMP
  Fitting with Xiao code
Magnetic Field Studies
Conclusions

## Slide 23: Fitting with Xiao Code
Xiao et. al. developed a code to include field dependence in BCS theory using an extension of Mattis-Bardeen theory
Using low field material parameters obtained from SRIMP fitting, the full field dependence of the BCS resistance can be computed at different temperatures
B. P. Xiao et. al. Superconducting surface resistance under radiofrequency field. Physica C, 490(0):26–31, 2013.

## Slide 24: Fitting with Xiao Code
Good agreement at medium fields

## Slide 25: Fitting with Xiao Code
Poor agreement at medium and high fields

## Slide 26: Fitting with Xiao Code
Xiao code can accurately predict behavior of BCS resistance at medium fields in Nitrogen-doped cavities
Theory deviates from observed behavior at low fields:
  The theory predicts a much more drastic increase in BCS resistance than we observe

## Slide 27: Outline
Deconvolution of Rres and RBCS
Fitting of field dependent data:
  Exponential fitting
  BCS fitting with SRIMP
  Fitting with Xiao code
Magnetic Field Studies
Conclusions

## Slide 28: Flux Trapping Studies
Temperature Sensors
Fluxgate
Magnetometer
Helmholtz
Coil
Slow Cool
Down System

## Slide 29: Fluxgate Measurements
External Field Off
External Field Off,
Flux Trapped
External Field On
TC

## Slide 30: Sensitivity to Trapped Magnetic Flux
A total of 10 cavity preparations were tested, each with different mean free paths – N-doping gives us the tools needed to finely tune the mean free path

## Slide 31: Sensitivity to Trapped Magnetic Flux
In the clean limit, longer mean free path leads to lower sensitivity of Rres to trapped magnetic flux
In the dirty limit, shorter mean free path leads to lower sensitivity
See our paper on ArXiV for full details: Gonnella et. al. arXiv:1509.04127
Notes: At low mfp, mean spacing between pinning sites decreases so sensitivity decreases. At high mean free paths, mean spacing no longer plays a roll so losses go as 1/mfp^1/2

## Slide 32: Sensitivity to Trapped Magnetic Flux
This is well described by theoretical predictions proposed by Alex Gurevich (Physical Review B, 87(5):054502, 2013.)
See our paper on ArXiV for full details: Gonnella et. al. arXiv:1509.04127
2
λ
l
H(t)
u(z,t)
This model is heavily dependent upon mean spacing between pinning sites: we assume a linear relationship between this mean free path
Notes: At low mfp, mean spacing between pinning sites decreases so sensitivity decreases. At high mean free paths, mean spacing no longer plays a roll so losses go as 1/mfp^1/2

## Slide 33: Outline
Deconvolution of Rres and RBCS
Fitting of field dependent data:
  Exponential fitting
  BCS fitting with SRIMP
  Fitting with Xiao code
Magnetic Field Studies
Conclusions

## Slide 34: Conclusions
Medium field Q slope in 120oC cavities is caused by a combination of increasing BCS and residual resistances
Anti-Q slope in Nitrogen-doped cavities is caused purely by decreasing BCS resistance
This anti-Q slope can be explained in a variety of ways: decreasing A or increasing ε in exponential fitting and increasing ε/kBTc in full BCS fitting
  Changing mean free path cannot solely explain the anti-Q slope since low field mean free paths are on either side of the minimum in N-Doped cavities

## Slide 35: Conclusions
Xiao code, a field-dependent derivation of Mattis-Bardeen theory can accurately predict BCS resistance at medium fields from low field material parameters but fails at low fields
Losses due to ambient magnetic fields are heavily dependent on mean free path and are very well explained by Gurevich’s theory of vortex oscillations