## Slide 1: Effects of External Magnetic Field on Cavity Performance
Dan Gonnella
Matthias Liepe
Cornell University

## Slide 2: The Experiment
A single-cell ILC shaped cavity was prepared with nitrogen doping at FNAL.
The cavity was placed inside a Helmholtz coil so that a uniform (parallel to cavity axis) magnetic field could be applied.
Trapped flux from the external field and residual resistance were measured for a variety of cool down rates.
Measurements were repeated on a standard EP+120oC baked cavity.

## Slide 3: Experimental Setup
Temperature Sensors
Fluxgate
Magnetometer
Helmholtz
Coil
Slow Cool
Down System

## Slide 4: Fluxgate Measurements
External Field Off
External Field Off,
Flux Trapped
External Field On
TC

## Slide 5: Q vs Temperature
18 cool downs with a variety of external magnetic fields and cool down rates.
Spread in Q0 at low temperature is caused by different residual resistance depending on cool down and applied external field.

## Slide 6: BCS Resistance vs Temperature
BCS Resistance remains unchanged regardless of cool down rate or external magnetic field – resistance from trapped flux is independent of temperature.

## Slide 7: Rres vs Accelerating Field
Residual resistance from trapped flux is independent of accelerating field.
Bexternal = 10 mG

## Slide 8: N2 Doped: Rres vs Cool Down Rate
Higher applied magnetic field yields higher residual resistance.
Faster cool down rate yields less residual resistance.
For more information see my other talk in WG8: “Cavity Testing for High Q0”

## Slide 9: Residual Resistance from External Field vs. Trapped Flux
Amount of flux trapped depends on cool down rate and external field applied.
Initial results suggest that residual losses from trapped flux are much higher (5X) in a N2 doped cavity than a EP+1200C baked cavity.

## Slide 10: Conclusions
Residual resistance decreases with faster cool down in both N2 doped and EP+120oC baked cavities as initially found by FNAL.
  Resistance from trapped flux is independent of both temperature and cavity field strength.
Residual losses from trapped flux is very different for the two cavities: the N2 doped cavity showed 2.9±0.2 nΩ/mG trapped and the EP+120oC cavity showed 0.6±0.1 nΩ/mG trapped.
Future work will focus on repeating this study on more cavities prepared in different ways:
  Additional N2 doped cavities, more cool downs on the EP+120oC cavity, EP, and BCP cavities.