## Slide 1: Cavity Testing for High Q
Dan Gonnella
Matthias Liepe
Cornell University

## Slide 2: The Experiment
A. Romanenko saw an improvement in Q with fast (>few K/min) on N2 doped and EP+120oC baked cavities.
Two single-cell ILC shaped cavities were tested with fast (>5 K/min) and slow (<<1 K/min) cool down.
  N2 doped cavity (prepared at FNAL by A. Grassellino)
  EP+120oC baked cavity
Q vs Temperature was measured for each cool down and residual resistance was extracted.
For the N2 doped cavity, Q vs E was measured at 2 K.

## Slide 3: N2 Doped: Q vs E at 2 K
Fast Cool Downs
Slow Cool Downs
Q0 increases from 1.5x1010 to 4x1010

## Slide 4: N2 Doped: Q vs Temperature
Fast Cool Downs
Slow Cool Downs
Cool Down Speed | Average Rres [nΩ]
Fast (>5 K/min) | 1.9
Slow (<<1 K/min) | 6.5

## Slide 5: N2 Doped: Residual Resistance
Residual resistance decreases with faster cool down speed.

## Slide 6: N2 Doped: BCS Resistance
Anti-Q slope is caused by decreasing BCS resistance which is unaffected by cool down speed
Note: Errors are approximately 20% on RBCS

## Slide 7: EP+120oC: Q vs Temperature
Cool Down Speed | Rres [nΩ]
Fast (>5 K/min) | 3.0
Slow (<<1 K/min) | 3.6
Fast: 8x1010
Slow: 6x1010

## Slide 8: N2 Doped Cavity in External Magnetic Field
Cavity was placed in a Helmholtz coil with field parallel to cavity axis.
3 different fields were applied and residual resistance was measured at different cool down rates for each field.
For more details see my other talk in WG7: “Effects of External Magnetic Field on Cavity Performance”
Applied Field [mG] | Normalized Slope [nΩ/(K/min)/nΩ]
0 | -0.03 ±0.02
10 | -0.02 ±0.01
20 | -0.038 ±0.007

## Slide 9: EP+120oC Baked Cavity in External Magnetic Field
Normalized Slope:
-0.010 ±0.005
EP+120oC cavity is less susceptible to residual losses from magnetic field.
Faster cool down rate gives less residual for both cavity treatments.
More cool downs with other external fields are needed.

## Slide 10: Conclusions
For N2 Doped cavities, fast cool down results in a significantly less Rres (75% lower) than slow cool down.
For the EP+120oC cavity in vertical test, fast cool down results in a slightly lower Rres (20%) than with slow cool down.
N2 doped cavities are more susceptible to residual losses from external magnetic field than EP+120oC baked cavities – see “Effects of External Field on Cavity Performance” in WG7 .
Future work will focus on continued studies on cavities with other preparations (EP, BCP).