## Slide 1: Update on Nitrogen Doping at Cornell
Dan Gonnella
TTC Meeting
December, 2014

## Slide 2: Nitrogen-Doping at Cornell
  Nitrogen-doping was first proposed at FNAL.
  The Cornell recipe, focusing on strong doping:
    Given 800oC in vacuum for 3 hours followed by 20 minutes in 60 mTorr of N2 followed by 30 minutes in vacuum.
    Applied to 5 single-cells and given differing amounts of final EP to study how performance changes with depth.
    Additionally applied to 5 9-cells.
Notes: Plot of pressure

## Slide 3: Cavity Preparation
Cavity | Treatment | Final EP [µm] | Quench Field [MV/m] | Q0(2 K, 16 MV/m)
TE1-1 | Standard N-Doping | 18 | 19 | 3.5x1010
TE1-2 | Standard N-Doping | 6 | 17 | 4x1010
TE1-3 | Standard N-Doping | 12 | 35 | 4.5x1010
TE1-4 | Standard N-Doping | 24 | 36 | 3.5x1010
TE1-5 | Standard N-Doping | 30 | 27 | 3x1010
TE1-1 | Argon Doping | 0 | 24* | 1.9x1010
TE1-4 | Standard N-Doping + 120oC Bake | 24 before bake | 18 | 3.6x1010
Average first pass quench field: 27 MV/m
Average first pass Q0(2 K, 16 MV/m): 3.7x1010
For reference LCLS-II specification is a Q0 of 2.7x1010 at 16 MV/m and 2.0 K.

## Slide 4: Q0 vs E: Single-Cells (first-pass)

## Slide 5: Sample Analysis
A sample treated with the cavities was analyzed using SIMS.
Nitrogen was found to be present above the background at least 50 µm into the material.

## Slide 6: Argon Doping
Quench is suspected to be fundamental to the cavity
Argon doping produces significantly worse Q0 than nitrogen-doping
There was no discernable difference in Q0 between the argon doping and standard cavity preparation.
Notes: Two slides comparing cavities

## Slide 7: Nitrogen Doping + 120oC Bake
120oC bake resulted in a slight increase in Q0.
Also resulted in a strong degradation in the quench field.
Notes: Two slides comparing cavities

## Slide 8
N-Doped 9-cell | 1st Pass EP [µm] | 2nd Pass Additional EP [µm] | Qo at 16MV/m, 2K | Quench | Status
AES018 | 14 | 10 | 2.3E10 (2nd) 3.2E10 (3rd) | 28MV/m 21MV/m | FE (onset 10MV/m) Quench
AES022 | 14 | 0 (re-HPR) | 2.0E10 (1st) 3.4E10 (2nd) | 24MV/m 17MV/m | FE (onset 8MV/m) Quench, FE free
AES023 | 17 | 10 | 3.4E10 (1st) 3.0E10 (2nd) | 14MV/m 16MV/m | Quench, FE free Quench, FE free
AES029 | 27 | None | 2.7E10 | 15MV/m | Quench, FE free
AES030 | 26 | 0 (re-HPR) | 2.7E10 (1st) 3.0E10 (2nd) | 17MV/m 16.6MV/m | Quench, leak at 1.8K Quench, FE free
Cavity Preparation
Average quench field: 18 MV/m
Average Q0(2 K, 16 MV/m): 3.2x1010
For reference LCLS-II specification is a Q0 of 2.7x1010 at 16 MV/m and 2.0 K.

## Slide 9: Q0 vs E: 9-Cells
All 9-cells meet or exceed LCLS-II Q0 specification!

## Slide 10: Conclusions and Outlook
Nitrogen-doping at Cornell has repeatedly shown Q0’s higher than 3x1010 at 2.0 K.
We have developed a recipe that results in quench fields > 25 MV/m in single-cells.
Average quench fields and Q0 significantly exceed LCLS-II specifications in single and 9-cells.
Argon doping caused no significant improvement compared with standard treatments.
Future work will focus on looking at additional treatments including doping with gases other than nitrogen and argon.

## Slide 11
Thanks for your attention!